Heat resistant inorganic paints

Hanoi University of Science and Technology, No: 01, Dai Co Viet Street, Hanoi, Vietnam

PRODUCT DESCRIPTION

INOR - PAINT BKV is heat resistant up to 1000°C and Zero VOC. Very good adhesion on iron, steel and aluminium.

APPLICATION

It is applied for stoves and industrial parts that will be stressed by high temperatures.

TECHNICAL SPECIFICATIONS
(TCCS 01: 2014/ĐHBK)

| SPECIFICATIONS | Unit | Value |
| --- | --- | --- |
| 1. Color | Samples | As samples |
| 2. Adhesion | point | ( 1 |
| 3. Drying time to thickness coating film at 23 ( 2oC | min | 25 - 40 |
| 4. Solid content | % | ( 40 |
| 5. Viscosity by flow cup VZ4 at 25 ( 1oC | second | 20 - 25 |
| 6. Flexibility | mm | 1 - 2 |
| 7. Hardness of the film | kG.cm | ( 20 |
| 8. Temperature resistance at 10000C | min | ≥ 120 |
| 9. Specific gravity | g/cm3 | 1.5 - 1.6 |
| 10. Theor. covering rate (at 20μm dry layer thickness) | g/m2 | ( 70 |

Surface preparation

All surfaces should be clean, dry and free from contamination.

Bare steel

Roughness: using abrasives suitable to achieve grade Fine to 30-85 μm.

Other surfaces

The coating may be used on other substrates. Please contact us for more information.

Condition during application

The temperature of the substrate should be maximum 35ºC. Temperature and relative humidity measured in the vicinity of the substrate. Good ventilation is usually required in confined areas to ensure correct drying.

Avoid contact with water or vapour when the coating film still wet.

Application methods

Spray Use airless spray or conventional spray

Brush Recommended for stripe coating and small areas, care must be taken to achieve the specified dry film thickness.

Storage

The product must be stored in a dry, cool, well ventilated space and away from source of heat and ignition. Containers must be kept tightly closed.

Handling

Handle with care. Stir well before use.

Packing size

1 kg; 5 kg; 10 kg; 15 kg; 20 kg; 25 kg; 50 kg and 100 kg containers. Packing may vary from requirements.

Disclaimer

The information in this data sheet is given to the best of our knowledge based on laboratory testing and practical experience. However, as the product is often used under conditions beyond our control, we cannot guarantee anything but the quality of the product itself.

Contact Add: Prof.Dr. La The Vinh, Hanoi University of Science and Technology (HUST)

Email: vinh.lathe1@hust.edu.vn; Mobile: 0912.540.041

Website: sonbkv.vn

# Text boxes

INOR - PAINT

BKV

TECHNICAL DATA SHEET